Synthesis of nanographene on Ni(111)
M. Olle et al., Nano Letters 12 (2012)
Synthesis of graphene nanoislands on Ni(111)
3. Post-annealing: nanoislands shape modification/selection
1. Propene/ethylene adsorption on Ni(111)
2. Cracking and irregular nanoislands growth
t
T
Dosing
450-500ºC
500-650ºC
500ºC
550ºC
600ºC
650ºC
450ºC
irregular clusters
truncated triangles
triangles
hexagons
[Speaker Notes: Talk of single-annealing? (maybe mention) Change images to b/w images from thesis]

---
Stacking, domains and domain boundaries
Stacking configurations
Rotated domains
top-fcc
top-hcp
bridge-top
Rotated
1. Synthesis of graphene nanoislands on Ni(111)
Topological defect boundaries
Type A: linear
Type B: circular
(1,3)
(1,3)
→ conductive
→ insulating..?
2.4 nm
28º
22º
31º
Rotational angle statistics
Yazyev et al., Phys. Rev. B 81 (2010)
Defect boundaries energetics
Confines resonances in Gr/SiC
E. Cockayne et al., Phys. Rev. B, 83 (2011)
[Speaker Notes: We have investigated the system quite deeply but I won’t have time to go into all the details, which may not be so interesting to you, so I’ll just give an overview. We have looked into the stacking configurations by resolving the atomic structure of Gr and Ni at the same time, and looked into the energetics of the different stackings, found a shifting mechanism, etc. More in particular we have studied the rotated domains, analyzed their relative angle and related the statistics to energetics of the domain boundaries...so from this it seems that the boundary energetics selects the rotated domains! We also looked at the topological defect boundaries, and found they’re essentially of two types, linear and circular. Theory tells us that the linear ones we found are transparent/conductive, while for the circular ones don’t know the exact electronic properties but we know they can confine resonances]

---
Spectroscopy: electronic decoupling of Gr
Lower shift => lower Gr-metal coupling
Visually (surface state)
Gr/Ni: reflection at Gr edges
-100mV
-150mV
Gr/Au: propagation under Gr
Energy shift
Bare metal
Graphene/Au
Graphene/Ni
0.2eV
2.4eV
Energy shift
Bare metal
Graphene/Au
Graphene/Ni
1.1eV
Image potential state (n=2) energy shift:
0.6eV
Surface state energy shift:

---
GNIs: scattering (QPI)
Inverse FFT:
Brihuega, et al., PRL 101 (2008)
Dirac cones recovered; doping (estimated): 150 mV
2. Intercalation of Au
Fast Fourier Transform:
2.44Å
4.36Å
q
Topo, Vb= 25mV
Atomic structure
Scattering patterns
K
K’
Γ
Reciprocal space:
Brihuega et al., PRL 101 (2008)
k̅1
k̅2
q
Quasi Particle Interference:
Reciprocal space: